Rough lumber of coniferous species.
Interpretation of Russian export grading rules in accordance to GOST 26002-83

1. Dimensions:

1.1 Sawn lumber is subdivided:

By thickness: Thin 16 - 22 mm Medium 25 - 44 mm Thick 50 - 100 mm

By width: Narrow 75 - 125 mm Wide 150 mm and wider

By length: Short 450 - 2400 mm Long 2700 - 6300 mm

1.2. Nominal thickness and width are guided by standard GOST 24454-80, where thickness of the lumber shall not exceed 100 mm.

1.3. Lengths of lumber are ranged:
from 1500 mm and up with a step of 300 mm;
from 450 mm up to 1350 mm with a step of 150 mm;
Lumber with length from 450 mm up to 1350 mm is manufactured by an order of State foreign trade organization.

1.4. Nominal dimensions of lumber are established for the wood of MC (moisture content) 20%. With MC of more or less than 20%, actual thickness and width of lumber shall be more or less than nominal dimensions in correlation with shrinkage value according to standard GOST 6782.1-75.

1.5. Limiting deviations from nominal dimensions of lumber shall not exceed in mm:

| By length | + 25 | - 12 |
| --- | --- | --- |
| By width | + 3 | - 2 |
| By thickness: |  |  |
| thickness less than 50 mm | + 2 | - 1 |
| thickness 50 mm und up | + 3 | - 2 |

Volume of lumber with maximum admitted deviations shall not exceed 25% of total volume of lumber.

2. Technical Requirements

2.1. Lumber shall be manufactured in accordance to the requirements of the present technology standard for the wood of Pine, Spruce, Fir and Larch species.

2.2. Lumber is subdivided by quality of the wood and by its machining into 1, 2, 3, 4 and 5 grades.

2.3. Lumber is arranged:
By dimensions;
By species;
By grades:

U/S Unsorted (combining 1, 2, 3 grades together, the percentage correlation of which shall correspond to the natural recovery of lumber while sawing);

4 grade separately;

5 grade separately;

Up to 15% of Fir is admitted in a load of Spruce lumber.

2.4. MC moisture content of lumber shall not exceed 22%. Variation of the moisture content is admitted by custom orders.

2.5. Antiseptic treatment of lumber is per standard GOST 10950-78.

2.6. Quality of the wood and manufacture of lumber shall correspond to the requirements specified in tables 1-3.

Pine and Larch Lumber                                                                                                                          Table 1

| Wood defects | Limiting norms of wood defects by grades |
| --- | --- |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 1. Knots 1.1. Intergrown knots 1.1.1. Round and Oval 1.1.1.1. Face | Admitted on outside face in dimensions in mm and number in pieces on average per 1000 mm of length of lumber. |
|  | In thick wide sawn lumber |
|  | 13-17 | 1 | 18-27 | 1 | 28-38 | 2 | Admitted |
|  |  |  |  |  | over 38 up to 50 | 1 |  |
|  | In thick narrow lumber |
|  | 10-14 | 1 | 15-24 | 1 | 25 | 2 | Admitted |
|  |  |  |  |  | over 25 up to 38 | 2 |  |
|  | In medium wide lumber |
|  | 10-14 | 1 | 15-18 | 1 | 19-25 | 3 | Admitted |
|  |  |  |  |  | over 25 up to 38 | 1 |  |
|  | In medium narrow lumber |
|  | 10-14 | 1 | 15-18 | 1 | 19-25 | 3 | Admitted |
|  |  |  |  |  | over 25 up to 32 | 1 |  |
|  | In thin lumber |
|  | 10-14 | 1 | 15-18 | 1 | 19-22 | 2 | Admitted |
|  |  |  |  |  | over 22 up to32 | 1 |  |
|  | In lumber of 75 mm wide knots shall not exceed: |
|  | 1/4 | 1/3 | 1/2 | 2/3 | Admitted |
|  | of face width |
|  | Number of knots on the inside face of lumber of 1 & 2 grades is admitted twice more and in 3 grade one and a half times more than for outside face. |
| 1.1.1.2. Edge & corner | Admitted on each edge with dimensions in mm and number in pieces for entire length of a piece: |
|  | In thick lumber: |
|  | up to 6 | 3-4 | 7-12 | 3-5 | 13-16 | 5-8 | Admitted |
|  |  |  | 13-19 | 3-5 | over 16 up to 25 | 3-5 |  |
|  |  |  |  |  | over 25 up to 32 | 3 |  |
|  | In medium lumber: |
|  | up to 6 | 2-3 | 7-12 | 2-4 | 13-16 | 2-4 | Admitted |
|  |  |  | 13-19 | 2-3 | over 16 up to 3/4 of thickness | 2-4 |  |
|  | In thin lumber: |
|  | up to 6 | 1-2 | 7-10 | 1-2 | up to 2/3 of thickness | 2 | Admitted |
| 1.1.1.3. End | Admitted on each end with dimensions in mm and number in pieces: |
|  | Not admitted | 25 | 1 | Admitted |
| 1.1.2. Spike, branchy including appeared on corners, and edge | Admitted on the inside face of sawn timber (lumber) in total number of intergrown round and oval knots with dimensions and amount as per paragraphs 1.1.1.1.; 1.1.1.2. |
|  | Dimension of knots in mm by maximum diameter is admitted of not more than: |
|  | 38 | 50 | admitted |
|  | Appearing of knots on edges: |
|  | Admitted with appearing on edge of not more than: |
|  | Not admitted | 1/4 of the thickness | 1/3 of the thickness | Admitted |
| Wood defects | Limiting norms of wood defects by grades |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 1.2. Encased sound, unsound, decayed, rotten 1.2.1. Face | Admitted on the outside face within the amount of intergrown sound knots with dimensions in mm and number in pieces in average per 1000 mm of the length of lumber: |
|  | In thick wide sawn timber lumber |
|  | Not admitted | 25 | 1 | 63 | 1 | Admitted Knot holes shall not exceed 32 mm in narrow and 38 mm in wide sawn timber (lumber) |
|  |  | Through the board unsound, decayed and rotten |  |
|  |  | Not admitted | 25 | 1 |  |
|  | In thick narrow lumber |  |
|  | Not admitted | 19 | 1 | 50 | 1 |  |
|  |  | Through the board unsound, decayed and rotten |  |
|  |  | Not admitted | 25 | 1 |  |
|  | In medium wide lumber |  |
|  | Not admitted | 19 | 1 | 50 | 1 |  |
|  |  | Through the board unsound, decayed and rotten |  |
|  |  | Not admitted | 19 | 1 |  |
|  | In medium narrow lumber |  |
|  | Not admitted | 13 | 1 | 38 | 1 |  |
|  |  | Through the board unsound, decayed and rotten |  |
|  |  | Not admitted | 19 | 1 |  |
|  | In thin lumber |  |
|  | Not admitted | Only sound |  |
|  |  | 13 | 1 | 38 | 1 |  |
|  |  |  |  | Through the board unsound, decayed and rotten |  |
|  |  |  |  | 19 | 1 |  |
|  | In lumber of 75 mm wide of all thickness the knot's sizes shall not exceed: |
|  | Not admitted | 1/3 | 1/2 | 2/3 |
|  |  | Of width of face |
| 1.2.2. Edge and corner, including knot holes | Admitted on each edge with dimensions in mm and by number in pieces on the entire length of lumber. |
|  | In thick lumber |
|  | Not admitted | 13 | 1-2 | 38 | 2-4 | Admitted |
|  | In medium lumber |
|  | Sound only |
|  | Not admitted | 10 | 1-2 | 32 | 2-4 | Admitted |
|  | In thin lumber |
|  | Sound only |
|  | Not admitted | 6 | 1-2 | 25 | 2-4 | Admitted |
|  | Knot holes not more than: |
|  | Not admitted | Admitted with depth not more than: | Admitted |
|  |  | In thick - 1/4 | thickness of lumber with showing on outside face not more than 2,0 mm | Admitted |
|  |  | In medium - 1/3 |  |  |
|  |  | In thin - 1/2 |  |  |
|  |  | Of thickness of lumber |  |  |
| Wood defects | Limiting norms of wood defects by grades |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 1.2.3. End | Not admitted | Admitted |
| 2. Checks 2.1. Side checks 2.1.1. Face checks 2.1.1.1. Non through | Admitted with extent of not more than: | Admitted by conditions of integrity of lumber |
|  | 1/3 | 1/2 | 2/3 |  |
|  | Of the length of lumber |  |
|  | Without appearing on ends and edges | With appearing on one end up to 1/3 of thickness without exiting from end to edge. |  |
| 2.1.1.2. Through 2.1.1.2.1. Through without appearing on the end, including ring shakes Note: | . |
|  | Not admitted | Admitted without exiting on edges from outside and inside faces with length of not more than: | Admitted by conditions of integrity of lumber |
|  |  | In thick lumber |  |
|  |  | 1/5 (1/2) | 1/3 (2/3) |  |
|  |  | Of the length of a piece |  |
|  |  | In medium lumber |  |
|  |  | 1/10 (1/4) | 1/5 (1/3) |  |
|  |  | Of the length of lumber |  |
|  | In thin lumber |
|  | Not admitted |
|  | Check sizes, shown without brackets, relate to outside face; those in brackets relate to inside face. |
| 2.1.1.2.2. Through appearing on end | Admitted with extension from each end of not more than, mm: |
|  | 30 | 40 | 50 | Width of lumber | 600 |
| 2.1.2. Edge checks | Admitted: |
|  | Shallow, length not more than 40 mm | Not crossing corners of edge | Admitted |
| Wood defects | Limiting norms of wood defects by grades |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 2.2. End checks | .. |
| 2.2.1. Heart checks | Heart checks | Admitted in thick lumber on one end with length extent not more than 1/2 of width of a piece | Admitted |
| 2.2.2. Ring shakes | Not admitted | Admitted with diameter of not more than, mm: In lumber with width 25 to 44mm – 10 45 to 63mm – 19 above 63mm – 25 | Admitted by conditions of integrity of lumber |
| 3. Defects of wood structure | . |
| 3.1. Slope of grain | Admitted, if grain deviation from straight direction per 300 mm of length of lumber compose not more than, mm: | Admitted |
|  | 10 | 19 | 25 |  |
| 3.2. Compression wood | Admitted without splits on ends | Admitted |
| 3.3. Pitch pockets Note: | On faces | Admitted |
|  | In thick lumber |  |
|  | Admitted non through with width not more than, mm: |  |
|  | 3 | 3 | 6 |  |
|  | With length up to, mm: |  |
|  | 75 | 100 | 200 |  |
|  | On each face in amount in pieces of not more than: |  |
|  | 2-3 | 4-6 | 8 |  |
|  | In medium and thin lumber |  |
|  | Admitted non through with width not more than, mm: |  |
|  | 3 | 3 | 6 |  |
|  | With length up to, mm: |  |
|  | 25 | 75 | 125 |  |
|  | On each face in amount in pieces of not more than: |  |
|  | 2-3 | 3-4 | 5 |  |
|  | Without appearing on edges and ends | - |  |
|  | Indicated amount of pitch pockets is admitted in less numbers on outside face and more numbers on inside face. |
|  | On edges | Admitted |
|  | Not admitted | Admitted |  |
|  |  | 1/2 of norm for outside face | Width up to 3 mm; length up to 100 mm in amount up to 4 pieces on each edge |  |
|  | On ends |  |
|  | Not admitted | Admitted in medium and thin lumber with width up to 3 mm and length up to 1/3 of width of lumber |  |
| Wood defects | Limiting norms of wood defects by grades |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 3.4. Pith Note: | Admitted in lumber of over 25 mm thick (without ring shakes and checks) | Admitted | Admitted |
|  | With extent up to 1/2 of length of lumber appearing on one end at distance not more than 1/6 of thickness of timber from inside face. | With extent of total length of lumber appearing on one end at distance not more than 1/4 of thickness from inside face. |  |  |
|  | Admitted in lumber of 25 mm thick and thinner |
|  | Not admitted | Admitted attached to inside face with appearing on outside face. | Admitted |
|  | In a load of lumber of 3 grade not more than 30% of boxed heart is admitted |
| 3.5. In bark (Bark pockets) | Not admitted | Admitted on faces non through not more than 25 mm wide in amount of 1 piece up to 75 mm long and up to 3 pieces with length up to 50 mm; On edges 2 pieces up to 2 mm wide, not more than 15 mm long; not admitted on ends. | Admitted up to 50 mm wide; In thick lumber on one face with no limit length. In medium and thin lumber up to 175 mm long. | Admitted |
| 3.6. Pitch & Pitch Streaks | Not admitted | Admitted on faces and edges in form of spots and streaks | Admitted |
| 4. Fungal defects | . |
| 4.1. Fungal heartwood stains (streaks) | Not admitted | Admitted in thick lumber on face or edge without appearing on ends up to 1/5 of width and length of a piece. Not admitted in medium and thin lumber | Admitted on faces and edges up to 1/2 of width and length of lumber, admitted showing on end with covering of not more than 10% of end’s area. | Admitted |
| 4.2. Light fungal sap stains and mold | . |
| 4.2.1. Surface | Not admitted | Admitted on faces and edges up to 2 mm deep in shape of spots and streaks with total area of covering of not more than 15% of area of one face. | Admitted on faces and edges in shape of spots and steaks. | Admitted |
| 4.2.2. Deep Note: | Not admitted | Admitted on faces and edges up to 2 mm deep in shape of spots and streaks with total area of covering of not more than 5% of area of one face. | Admitted on faces and edges up to 2 mm deep in shape of spots and streaks with total area of covering of not more than 50% of area of one face and edges. With covering of not more than 10% of end area. | Admitted |
|  | Volume of lumber with maximum admitted norm of deep fungal sap stains in a batch of 4 grade shall not exceed 25%. |
| Wood defects | Limiting norms of wood defects by grades |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 4.3. Decay 4.3.1. Sap Decay | . |
|  | . |
| 4.3.1.1. Firm | Not admitted | In thick lumber is admitted on face or edge up to 1/5 of width and length without appearing on ends. Not admitted in medium and thin lumber | Admitted on faces and edges up to 1/2 of width and length of lumber without appearing on end. | Admitted |
| 4.3.1.2. Soft | Not admitted |
| 4.3.2. Heart Decay | Not admitted | Brown checked not admitted. Firm mottle honeycomb is admitted appearing on all sides in shape of streaks covering not more than 50% area of one face. Decay shall not cover more than 20% of and area. |
| 4.3.3. External rot | Not admitted |
| 5. Insect damages | . |
| 5.1. Wormholes | Not admitted | External is admitted, caused by bark beetles |

Spruce and Fir Lumber                                                                                                                          Table 2

| Wood defects | Limiting norms of wood defects by grades |
| --- | --- |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 1. Knots | Admitted on outside face in dimensions in mm and amount in pieces on average per 1000 mm of lumber length. |
| 1.1. Intergrown knots |  |
| 1.1.1. Round & Oval |  |
| 1.1.1.1. Face |  |
|  | In thick lumber |
|  | 13 | 3 | 19-25 | 3 | Admitted | Admitted |
|  | Over 13 up to 19 | 1 | Over 25 up to 38 | 2 | 70-75 | 1-2 on entire length |  |
|  | Over 19 up to 25 | 1 | Over 38 up to 50 | 1-2 on entire length |  |  |  |
|  |  |  | With absence of unsound, decayed, rotten knots | With absence of enlisted unsound, decayed, rotten knots |  |
|  | In medium lumber |
|  | 13 | 2 | 19-25 | 2 | 38-50 | 1 | Admitted |
|  | Over 13 up to 19 | 1 | Over 25 up to 37 | 1 | (over 50 up to 63) | 1 – 2 on entire length |  |
|  |  |  |  |  | With absence of unsound, decayed, rotten knots |  |
|  | In thin lumber |
|  | 13-18 | 1 | 19-31 | 1-2 | 32 | 3 | Admitted |
|  |  |  |  |  | (over 32 up to 38) | 1 |  |
|  |  |  |  |  | With absence of unsound, decayed, rotten knots |  |
|  | In lumber of 75 mm wide of all thickness size of knots shall not exceed: |
|  | 1/3 of face width | 1/3 of face width | 1/2 of face width | 2/3 of face width | Admitted |
| Note: | 1. Knots, dimensions of which are shown in brackets, admitted among recorded knots of smaller dimensions. 2. Quantity of knots on inside face is admitted: in 1 grade – double, in 2 grade – one and a half, in 3 grade – one time correspondently to norm for outside face. |
| Wood defects | Limiting norms of wood defects by grades |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 1.1.1.2. Edge & Corner | Admitted on each edge with dimensions in mm and number in pieces for entire length of lumber: |
|  | In thick lumber: |
|  | Up to 13 | 8 | 19-43 | 3-6 | 44-50 | 1-3 | Admitted |
|  | Over 13 up to 16 | 4 |  |  |  |  |  |
|  | Over 16 up to 18 | 1-3 |  |  |  |  |  |
|  | In medium lumber |
|  | up to 13 | 2-3 | From 14 up to 2/3 of thickness of timber | 2-3 | From 19 up to 3/4 of thickness of timber | 3-5 | Admitted |
|  | In thin lumber |
|  | Up to 6 | 2-3 | From 7 up to 12 | 1-2 | From 13 up to thickness of timber | 2-4 | Admitted |
| 1.1.1.3. End | Admitted with dimensions in mm and number in pieces: |
|  | On one end 1 knot up to 25 | On both ends 1 knot up to 25 | 25 | 1 | Admitted |
|  |  |  | On each end |  |
| 1.1.2. Spike, branchy including appeared on corners, and edge knots | Admitted on the inside face of sawn timber (lumber) in total number of intergrown round and oval knots with dimensions and amount as per paragraphs 1.1.1.1.; 1.1.1.2. In sawn timber of 1 grade largest diameter of branchy knot shall not exceed 50 mm and it shall not cover more than 1/4 of thickness of an edge. |
| 1.2. Encased sound, unsound, decaying, rotten | Admitted on each face within the amount of intergrown sound knots with dimensions in mm and number in pieces for the entire length of lumber: |
| 1.2.1. Face | In thick lumber |
|  | Not admitted | Up to 30 | 3-6 | Over 30 up to 50 | 3-6 | Admitted | Admitted. Knot holes shall not exceed 32 mm in narrow and 38 mm in wide lumber |
|  | Through the board unsound, decayed and rotten |  |
|  | Not admitted | Up to 38 | Admitted |  |
|  | In medium lumber |
|  | Not admitted | Up to 20 | 2-4 | Over 20 up to 25 | 2-4 | Admitted |
|  | Through the board unsound, decayed and rotten | Admitted |
|  | Not admitted | Up to 25 | Admitted |  |
|  | In thin lumber |
|  | Not admitted | Up to 16 | 1-3 | Over 16 up to 22 | 1-3 | Admitted |
|  | Through the board unsound, decayed and rotten | Admitted |
|  | Not admitted | Up to 25 | Admitted |  |
|  | In lumber with width of 75 mm and any thickness, dimension of knots shall not exceed: |
|  | Not admitted | 1/3 of the face width | 1/2 of the face width | Admitted |
| Wood defects | Limiting norms of wood defects by grades |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 1.2.2. Edge and corner, including knot holes | Admitted on each edge with dimensions in mm and number in pieces on the entire length of lumber |
|  | In thick lumber |
|  | Not admitted | Up to 15 | 1-2 | 16-25 | 2-4 | Admitted |
|  | In medium lumber |
|  | Not Admitted | 13-19 | 1-3 | Admitted |
|  | In thin lumber |
|  | Not admitted | 6-10 | 1-2 | Admitted |
|  | Knot holes on edges |
|  | Not admitted | Admitted covering up to: | Admitted |
|  |  | 2/3 of thickness of lumber | Entire thickness of lumber with appearing on outside face in extent of 2 mm |  |
| 1.2.3. End | Not admitted | Admitted |
| 2. Checks 2.1. Side Checks 2.1.1. Face 2.1.1.1. Non through |  |
|  | Admitted with extent of not more than: | Admitted by conditions of integrity of lumber |
|  | 1/3 | 2/3 | 3/4 |  |
|  | of the length of lumber |  |
|  | Without appearing on ends and edges | with appearing on one end up to 1/2 of thickness without exiting from end to edge. |  |
| 2.1.1.2. Trough 2.1.1.2.1. Through without appearing on the end, including ring shakes | Not admitted | Admitted on outside face and for ring shakes on inside face with length of not more than: | Admitted by conditions of integrity of lumber |
|  |  | 1/4 | 1/3 |  |
|  |  | Of the length of lumber |  |
| 2.1.1.2.2. Through appearing on end | Admitted with extension from each end of not more than, mm: |
|  | 50 | 75 | 100 | Width of a piece | 600 |
| 2.1.2. Edge checks | Admitted, mm: |
|  | Shallow, length not more than 75 mm | Not crossing corners of edge | Admitted |
| 2.2. End checks 2.2.1. Heart checks | Not admitted | Admitted in thick sawn timber on one end with length extent not more than 3/4 of width of a piece | Admitted by conditions of integrity of lumber |
| 2.2.2. Ring shakes | Not admitted | Admitted with diameter of not more than, mm: In sawn timber with width: 25 to 44mm – 10 45 to 63mm – 19 above 63mm – 25 | Admitted by conditions of integrity of lumber |
| Wood defects | Limiting norms of wood defects by grades |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 3. Defects of wood structure 3.1. Slope of grain | Admitted, if grain deviation from straight direction per 300 mm of piece’s length compose not more than, mm: | Admitted |
|  | 13 | 25 | 38 |  |
| 3.2 Compression wood | Admitted without splits on ends | Admitted |
| 3.3 Pitch pockets | On faces |
|  | Admitted on each face without appearing on edges and ends with width up to 3 mm and length not more than, mm: | Admitted not through up to 6 mm wide and up to 200 mm long in amount of 10 pcs. on each face | Admitted |
|  | 75 | 150 |  |  |
|  | In amount of not more than, pcs: |  |  |
|  | 3 | 5 |  |  |
|  | On edges |
|  | Admitted with dimensions and numbers not exceeding 1/2 of those stipulated for the face. | Admitted |
|  | On ends |
|  | Not admitted | Admitted in medium and thick sawn timber with width up to 3 mm and length up to 1/3 of width of lumber | Admitted |
| 3.4. Pith Note: | In lumber of less than 22 mm thick: |
|  | Not admitted | Admitted |
|  | In lumber of over 22 mm and up to 44 mm thick: |
|  | Admitted with extend of entire length of lumber with appearing on one or both ends not far from inside face than: | Admitted |
|  | 1/4 | 1/3 | 1/3 |  |
|  | Of thickness of lumber without checks and shakes in 1 and 2 grades. |  |
|  | In lumber of over than 44 mm thick: |
|  | Admitted with extend of entire length of lumber far from inside face not less than 1/4 of thickness of lumber | Admitted |
|  | In a load of sawn timber of 3 grade not more than 30% of boxed heart is admitted |
| 3.5. In bark (bark pockets) | Not admitted | Admitted on faces non through in amount up to 4 pcs in lumber with thickness of 55 mm and up: 125 mm long and 25 mm wide; in lumber with thickness of less than 55 mm: 63 mm long and 15 mm wide; On edges 2 pieces up to 2 mm wide, not more than 20 mm long; | Admitted |
| 3.6. Pitch & Pitch Streaks | Not admitted | Admitted on faces and edges in form of spots and streaks | Admitted |
| Wood defects | Limiting norms of wood defects by grades |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 4. Fungal defects 4.1. Fungal heartwood stains (streaks) | Not admitted | Admitted on face or edge up to 1/4 of width and length of lumber | Admitted on faces and edges up to 1/2 of width and length of lumber, admitted showing on end with covering of not more than 10% of end’s area. | Admitted |
| 4.2. Light fungal sap stains and mold 4.2.1. Surface | Not admitted | Admitted on faces and edges up to 2 mm deep in shape of spots and streaks with total area of covering of not more than 15% of area of one face | Admitted on faces and edges in shape of spots and steaks. Covering of not more than 10% of end’s area | Admitted |
| 4.2.2. Deep Note: | Not admitted | Admitted on faces and edges in shape of spots and streaks with total area of covering of not more than 5% of area of one face. | Admitted on faces and edges in shape of spots and streaks with total area of covering of not more than 50% of area of one face and edges. With covering of not more than 10% of end’s area. | Admitted |
|  | Volume of lumber with maximum admitted norm of deep fungal sap stains in a batch of 4 grade shall not exceed 25%. |
| 4.3. Decay 4.3.1. Sap decay 4.3.1.1. Firm | Not admitted | Admitted on face or edge up to 1/4 of width and length of lumber | Admitted on faces and edges up to 1/2 of width and length of lumber without appearing on ends | Admitted |
| 4.3.1.2. Soft | Not admitted |
| 4.3.2. Heart Decay | Not admitted | Admitted firm non through with dimensions up to 1/5 of width and length of lumber without appearing on ends | Admitted firm on one face with dimensions up to 1/4 of width and 1/3 of length of lumber, slightly exiting on another face and edges | Brown checked not admitted. Firm mottle honeycomb is admitted appearing on all sides in shape of streaks covering not more than 50% area of one face. Decay shall not cover more than 25% of end’s area |
| 4.3.3. External rot | Not admitted |
| 5. Insect damages 5.1. Wormholes | Not admitted | External is admitted, caused by bark beetles |
| Note: Table 1 & 2 | 1. Amount of knots for entire length of lumber, shown “from – to” means that less amount is admitted for short lumber and more – for long. 2. Knots with less dimensions than indicated are disregarded. 3. Intergrown knots could be knots fully intrgrown on one face and fully incased on another face or edge. 4. In U/S (1-3 grades together) lumber, simultaneous presence of incased knots, checks and fungus sapwood stains with maximum limits are not admitted. 5. With absence of other limiting defects one defect is admitted exceeding 20% of parameters, except for blue stain and checks. |

Table 3

| Wood defects | Limiting norms of wood defects by grades |
| --- | --- |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 1. Manufacturing defects 1.1. Wane |  |
| 1.1.1. Obtuse | Admitted on one edge with extension of not more than: | Admitted on both edges extended not more than 2/3 of the length of lumber | Admitted on both edges extended on entire length with covering of not more than 2/3 of thickness and width of lumber |
|  | 1/5 | 1/4 | 1/3 |  |  |
|  | Of the length of the lumber |  |  |
|  | On both edges: |  |  |
|  | 1/10 | 1/5 | 1/4 |  |  |
|  | Of the length of the lumber |  |  |
|  | Width of wane, calculated by maximum value of miss sawn part in mm, is admitted of not more than: |  |
|  | In lumber with thickness up to 25 mm: |  |
|  | 1/4 | 1/3 | 1/2 | 2/3 |  |
|  | Of thickness of lumber |  |
|  | In lumber with thickness over 25 mm: |  |
|  | 1/5 | 1/4 | 1/3 | 2/3 |  |
|  | Of thickness of lumber |  |
|  |  | Wane admitted on condition that sawn part of edge shall be not less than 1/2 of thickness of lumber |  |
| 1.1.2. Sharp | Not admitted | Admitted on one edge not more than 1/10 of length of lumber provided that nominal width of inside face shall be maintained |
| Note: | The wane shall be free of bark and inner bark, in lumber of 5 grade inner bark may be present |
| 1.2. Saw marks | The depth of saw teeth marks shall not exceed 0,75 mm |
| 1.3. Fringe | Not admitted |
| 1.4. Bevel cut | Declinations from perpendicularity of end to face and to edge are admitted up to 3% of width and thickness of lumber correspondently. |
| 1.5. Chipping | Chipping due to mechanical damages, saw kerfs, knife marks caused by debarking machines on edge corners next to inside face are not admitted; on edge corners next to outside face are admitted correspondently to wane limitations. |
| 1.6. Waving | The height of wave shall not exceed 0,75 mm |
| 1.7. Torn grain | On faces |
|  | Admitted not more than 0,75 mm deep without number limitations | Admitted up to 3 mm deep without number limitations | Admitted |
|  | On edges |
|  | Admitted not more than 3 mm deep without number limitations | Admitted not more than 5 mm deep without number limitations | Admitted |
| Note: | Limits for waving and torn grain are indicated only for lumber recovered on “chip and saw” equipment |
| 1.8. Foreign particles (nails, wire, metal debris and etc.) | Not admitted |
| Wood defects | Limiting norms of wood defects by grades |
|  | 1 grade | 2 grade | 3 grade | 4 grade | 5 grade |
|  | size | number | size | number | size | number | size | number | size | number |
| 2. Warping |  |
| 2.1. Crook | Admitted with deflection of not more than, % |
|  | 0,10 | 0,10 | 0,15 | 0,20 | admitted |
|  | Of the length of lumber |
| Note: | 1. Volume of lumber with admitted crook warp shall not exceed 20% of the total volume of the said grade. 2. Values for crook warp for lumber of different length are given in reference Annex |
| 2.2. Bow | Admitted with deflection per each 1500 mm of the length of lumber of not more than, mm: | Admitted |
|  | 2 | 4 | 6 | 13 |  |
| 2.3. Cup | Admitted with deflection of not more than, mm: | Admitted |
|  | For wide lumber |  |
|  | 3 | 3 | 6 | 10 |  |
|  | For narrow lumber |  |
|  | 1 | 1 | 3 | 6 |  |
| 2.4. Twist | Admitted with deflection from sawing plain not more than 13 mm for entire length of lumber | Admitted |
| Note: | Volume of lumber with crook, bow and twist, provided p. 2.2-2.4 shall not exceed in U/S grade - 10%, in 4 grade – 20% of total volume. |